## Slide 1: Thickness Measurement in TEM
EELS vs CBED

## Slide 2: Agenda
What possibilities exist?
A little bit bout EELS
A little bit bout CBED
Show-case Aluminum CBED
Show-case Aluminum EELS
Hints & “the program”
Possible & Planned Extensions of Program

## Slide 3: What possibilities exist?
FIB cross-section
Thickness-Fringes
Projected widths/ Planar Defects
EELS
KM- fringes (CBED)
…..
Williams & Carter

## Slide 4: A little bit bout EELS (Electron Energy-Loss Spectrometry)
Low energy-loss:
Zero-loss
Plasmons
Inter-Intraband transitions
High energy-loss:
Ionization edges
…
 Composition, band structure, specimen thickness, …..
EELS: Analysis of energy spectrum of transmitted electrons. Energy losses through:

## Slide 5: A little bit bout EELS (Electron Energy-Loss Spectrometry)
Spectrometers:
PEELS: Parallel- collection EELS
GIF: Gatan Imaging Filter
Ω: Omega Filter
EFTEM

## Slide 6: A little bit bout CBED (Convergent Beam Electron Diffraction)
Based on measuring Kossel and Möllenstedt fringes (K-M) in g spot
Theory described by Kelly & refined by Allen et al.
„[…] im Inneren der Scheiben aber zeigen sich Intensitätsschankungen, die von der merklich gewordenen Ausdehnung des Gitters in die Tiefe Herrühren.“ –Kossel 1939
Interesting artikle on CBED and Nazis: https://blogs.kent.ac.uk/sciencecomma/2019/12/13/scientific-discovery-under-nazi-rule/
Möllenstedt’s auto-biography: https://sci-hub.se/https://doi.org/10.1016/S1076-5670(08)70060-0
Really easy to read paper „about everything“: https://sci-hub.se/https://doi.org/10.1016/S0031-8914(40)90101-X
Notes: MacGillavry
Staff and their families either went with the equipment on the SS Deutschland or via the Wilhelm Gustloff [30]. Both ships were heading to Kiel in Germany. Sadly, those who went via the Gustloff became part of the worst maritime disaster in history [31].
Built only to accommodate 1900 people, upwards of 10,000 people desperately packed onto the ship. The temperature outside was viscously cold, minus 18 degrees, so cold the life boats had frozen to the deck. Two of the ships accompanying the Gustloff had technical troubles and returned to Danzig, leaving only one torpedo boat. When a Soviet submarine encountered the Gustloff on the eve of January 30th, it was a sitting duck. Over 9000 people died.
SS Deutschland
Fortunately for Kossel and Möllenstedt, they decided to take the SS Deustchland

## Slide 7
A little bit bout CBED (Convergent Beam Electron Diffraction)
Sample thickness (t)
s = 0
Rocking- curve: Intensity distribution with the change of diffraction conditions due to dynamical diffraction.
K-M pattern
s0 s1 s2 s3
Δϴ1
Δϴ2
Δϴ3
Workflow:
Obtain CBED from 2-Beam Condition
Measure Δϴi
Calculate si
Plot Kelly’s equation
Change ni until linear
Kelly’s equation:
= ; ϵ ℕ
Allen

## Slide 8
A little bit bout CBED (Convergent Beam Electron Diffraction)
Workflow:
Obtain CBED from 2-Beam Condition
Measure Δϴi
Calculate si
Plot Kelly’s equation
Change ni until linear
Kelly’s equation:
= ; ϵ ℕ
y
x
m
y(x=0)
Williams & Carter

## Slide 9: Show-case Aluminum CBED
<200>
<220>
S1A3
S5A1

## Slide 10: Show-case Aluminum EELS
Values for λP taken from : https://www.researchgate.net/publication/259329092_Mean_free_path_of_inelastic_electron_scattering_in_elemental_solids_and_oxides_using_transmission_electron_microscopy_Atomic_number_dependent_oscillatory_behavior
λP Al : 160 nm
Area1
Area2
156.8 nm
128 nm
Cumulative with same e- count
337.6 nm
Cumulative vs. Calin’s 0.15 sec
270.4 nm
Thickness- through EELS:
20% accuracy ( original Paper)
GIF @2100: negative counts
GIF @2100: energy gain

## Slide 11: Hints & “the program”
Hint: Align TEM in spotsize 3 and use it for the BF/DF and CBED micrographs.
The higher R² value the better the fit
It takes sometimes more iterations, but trustworthy results should not exceed ~ 4 iterations
A nice CBED pattern doesn’t mean that they give nice results. Especially not if taken with poorely/not at all aligned conditions.
A perfect fit must be found to be able to extract the location of the g-spot in the rocking curve.
Hint: Align TEM in spotsize 3, condenser aperture 2 (70µm) and use it for the BF/DF and CBED micrographs.
Make sure that only 2 beams are excited to avoid faulty pattern!!!

## Slide 12: Possible & Planned Extensions of Program
Planned:
  - Writing an interactive Jupyter notebook
Possible:
  - Thickness range
  Allen’s refinement (taking additionally maxima locations)
  Comparing with/ retrieving extinction length
  Fully automation

## Slide 13
The End

## Slide 14: Nice-to-now
Allen 1981

## Slide 15: Tina’s Summary